ABSTRACT

RIANTO, Utilization Shells Ash as Substituted Most Cement With Addition Foam Agent Against Non-Structural Lightweight Concrete Characteristics. Essay, Jakarta: Department of Civil Engineering, Faculty of Engineering, State University of Jakarta. 2015.

Non-structural lightweight concrete is made from sand, cement, foam agent and ash shells as partial substitution of cement. This study aims to determine the ash addition of seashells on the compressive strength and flexural strength with a variation of 0%, 5%, 7.5% and 10% for the design of concrete quality 1.4 MPa.

This research was conducted at the Laboratory of biocomposite, Biomaterial Research Center, Indonesian Institute of Science (LIPI) with the experimental method. The test specimen used is a cylinder with a diameter of 3 inches and 6 inches high and tested for compressive strength using tools Compression Testing Machine (CTM). For the flexural strength test specimen used in the form of beams with a length of 16 cm, 4 cm wide and 4 cm high and tested using a Universal Testing Machine (UTM).

The results showed that there were differences in normal concrete and concrete with the addition of ash shells. Compressive strength and flexural strength optimum at 28 days occurred on addition of ash shells variation of 7.5% which is 1.54 MPa and 0.95 MPa. The use of ash shells as partial substitution of cement can increase the strength of lightweight concrete, but the higher ash content will be further reduced shells of concrete strength. This is because the high ash content of calcium oxide shells are just as accelerating admixture or accelerate the bonding time.

Keywords: Non-Structural Lightweight Concrete, Shells Ash, Foam Agent, Mechanical Properties.